A4 STOCK SPECIALITY SPEC SHEET

MULTIPURPOSE (LASER/COPIER PRODUCTS)

[image: image1.jpg]


[image: image2.jpg]



Translucent Paper with a permanent adhesive

(T)

A semi-transparent paper specifically designed for use on ‘hot fuse’ printer systems. Ideal for applications using variable information printing such as address & inventory labels where a natural no label look is required. Due to the high moisture content of the face material, some curl may occur on exiting the printer. This will flatten, but multi-fed sheets should be avoided.

Important Note: Due to the nature of this face material, special care must be taken when handling and printing to avoid poor toner adhesion. In particular only use original toner cartridges and ensure the machine is set for “Labels” or “Heavy card” stock. And ensure any and all unused sheets are returned to it’s bag and box for storage.

Face material properties 
Grammage



63 gsm

Caliper (thickness)


55 microns

Adhesive

A clear permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. 

Minimum application temp.

0(C

Storage range once applied

-20(C to +80(C

Backing

A one side clay coated, bleached kraft paper with good lay-flatness & stability

Thickness



110 microns 

Grammage



 98 gsm

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications but may vary. All products within our range are manufactured to ISO 9001:2015 and BRC standards, the factory is also PEFC and FSC certified. The raw material laminates are also made to the same ISO standards as above and to ISO 14001.
Markets and Uses
Used for sealing packages/boxes on small items.  Product gives a No Label Look so also used for mailing when the envelope/package is already decorative/coloured where a white label would look out of place.

Retail, Mail Houses, Product Labelling

Issue: 092019
